PRODUCT SPECIFICATION

PRODUCT SPECIFICATION

Preliminary

- P/N：PO-MT3535NWSN-D01

| CUSTOMER APPROVED SIGNATURES | APPROVED BY | CHECKED BY | PREPARED BY |
| --- | --- | --- | --- |

- Features

- Small package with high efficiency

RoHs Compliant and Pb-Free

- Energy Star / ANSI compliant binning structure

- Application

- Tiny illumination

- PAR 30 light bulb

- Spot light

- Indicator

- Absolute Maximum Ratings

（Ta=25℃）

| Parameter | Symbol | Rating | Unit |
| --- | --- | --- | --- |
| Max Pulse Power Dissipation | PD | 3 | W |
| Forward Current (DC) | IF | 700 | mA |
| Forward Voltage (DC) | VF | 3.6 | V |
| Reverse Current | IR | 85 | mA |
| Operating Temperature | Topr | -40 ~ +100 | ℃ |
| Storage Temperature | Tstg | -40 ~ +100 | ℃ |
| LED junction temperature | Tj | 120 | ℃ |

- Mechanical Dimension

Cathode Mark

Cathode Mark

(unit:mm)

Note:

- Dimensions are in millimeters.

- Tolerance +/- 0.2 mm.

- Luminous Flux Characteristics

（Ta=25℃）

| Color | CCT | Part No. | CRI | Luminous Flux (lm) |  |  | Condition |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Ra | Min | Type | Max |  |
| Natural White | 4000K | PO-MT3535NWSN-D01 | 80 | 90 | / | 140 | IF=350mA |

Note:

- Maintains a tolerance of ±10% on Luminous Flux measurements.

- Maintains a tolerance of ±2% on CRI measurements.

- Optical Characteristics

（Ta=25℃）

| Color | Part No. | Color Temperature |  |  | Typical View Angle (Degrees) 2θ ½ |
| --- | --- | --- | --- | --- | --- |
|  |  | Min. | Typ. | Max. |  |
| Natural White | PO-MT3535NW-D01 | 3710 | / | 4745 | 120∘ |

Note:

- Maintains a tolerances of ±5% for CCT measurements.

- Electrical Characteristics

Ta=25℃）

| Color | Part No. | Forward Voltage VF(V) |  |  | Condition |
| --- | --- | --- | --- | --- | --- |
|  |  | Min | Type | Max |  |
| Natural White | PO-MT3535NW-D01 | 2.9 | / | 3.6 | IF=350mA |

Note:

1.  Maintains a tolerance of ±1v on Forward Voltage measurements.

- Bin Range Of Luminous Intensity

| Bin | Min | Max | Unit | Condition |
| --- | --- | --- | --- | --- |
| AB | 90 | 100 | lm | IF=350mA |
| AC | 100 | 110 |  |  |
| AD | 110 | 120 |  |  |
| AE | 120 | 130 |  |  |
| AF | 130 | 140 |  |  |

- Bin Range Of Forward Voltage

| Bin | Min | Max | Unit | Condition |
| --- | --- | --- | --- | --- |
| H1 | 2.9 | 3.0 | V | IF=350mA |
| H2 | 3.0 | 3.1 |  |  |
| I1 | 3.1 | 3.2 |  |  |
| I2 | 3.2 | 3.3 |  |  |
| J1 | 3.3 | 3.4 |  |  |
| J2 | 3.4 | 3.5 |  |  |
| K2 | 3.5 | 3.6 |  |  |

- Typical Electro-Optical-Thermal Characteristics Curves

(TA=25℃ Unless Otherwise Noted)

| 1.Relative Luminous Flux vs. Forward Current | 2.Forward Voltage vs. Forward Current |
| --- | --- |
| 3.Relative Luminous Flux vs. Ambient Temperature | 4.Forward Voltage vs. Ambient Temperature |
| 5.Spectrum Distribution-CRI 80 | 6. Radiation Diagram |

- ANSI Chromaticity Bin Table

Natural White BIN Structure

Note :The red dashed circle is main bin

| Bin code | CIE-x | CIE-y |  | Bin code | CIE-x | CIE-y |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 45A | 0.3152 | 0.3465 |  | 40A | 0.3670 | 0.3578 |  |
|  | 0.3530 | 0.3601 |  |  | 0.3703 | 0.3726 |  |
|  | 0.3617 | 0.3663 |  |  | 0.3828 | 0.3803 |  |
|  | 0.3591 | 0.3522 |  |  | 0.3784 | 0.3647 |  |
| 45B | 0.3530 | 0.3601 |  | 40B | 0.3703 | 0.3726 |  |
|  | 0.3548 | 0.3736 |  |  | 0.3736 | 0.3874 |  |
|  | 0.3642 | 0.3805 |  |  | 0.3871 | 0.3959 |  |
|  | 0.3617 | 0.3663 |  |  | 0.3828 | 0.3803 |  |
| 45C | 0.3617 | 0.3663 |  | 40C | 0.3828 | 0.3803 |  |
|  | 0.3642 | 0.3805 |  |  | 0.3871 | 0.3959 |  |
|  | 0.3736 | 0.3874 |  |  | 0.4006 | 0.4044 |  |
|  | 0.3703 | 0.3726 |  |  | 0.3952 | 0.3880 |  |
| 45D | 0.3591 | 0.3522 |  | 40D | 0.3784 | 0.3647 |  |
|  | 0.3617 | 0.3663 |  |  | 0.3828 | 0.3803 |  |
|  | 0.3703 | 0.3726 |  |  | 0.3952 | 0.3880 |  |
|  | 0.3670 | 0.3578 |  |  | 0.3898 | 0.3716 |  |

Note:

Maintains a tolerances of ±0.01 on Color coordinates measurements.

- PACKAGING

PO-MT3535NWSN-D01 High Power LEDs are packaged in reel of 1000 paces and placed inside a carton.

LABEL

BIN CODE

Lot

Qty

LABEL

BIN CODE

Lot

Qty

Carton

CARTON