PRODUCT SPECIFICATION

PRODUCT SPECIFICATION

Preliminary

- P/N：PO-MT3535WWSN-D01

| CUSTOMER APPROVED SIGNATURES | APPROVED BY | CHECKED BY | PREPARED BY |
| --- | --- | --- | --- |

- Features

- Small package with high efficiency

RoHs Compliant and Pb-Free

- Energy Star / ANSI compliant binning structure

- Application

- Tiny illumination

- PAR 30 light bulb

- Spot light

- Indicator

- Absolute Maximum Ratings

（Ta=25℃）

| Parameter | Symbol | Rating | Unit |
| --- | --- | --- | --- |
| Max Pulse Power Dissipation | PD | 3 | W |
| Forward Current (DC) | IF | 700 | mA |
| Forward Voltage (DC) | VF | 3.6 | V |
| Reverse Current | IR | 85 | mA |
| Operating Temperature | Topr | -40 ~ +100 | ℃ |
| Storage Temperature | Tstg | -40 ~ +100 | ℃ |
| LED junction temperature | Tj | 120 | ℃ |

- Mechanical Dimension

Cathode Mark

Cathode Mark

(unit:mm)

Note:

- Dimensions are in millimeters.

- Luminous Flux Characteristics

（Ta=25℃）

| Color | CCT | Part No. | CRI | Luminous Flux (lm) |  |  | Condition |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Ra | Min | Type | Max |  |
| Warm White | 2700K | PO-MT3535WWSN-D01 | 80 | 80 | / | 130 | IF=350mA |
|  | 3000K |  |  |  |  |  |  |

Note:

- Maintains a tolerance of ±10% on Luminous Flux measurements.

- Maintains a tolerance of ±2% on CRI measurements.

- Optical Characteristics

（Ta=25℃）

| Color | Part No. | Color Temperature |  |  | Typical View Angle (Degrees) 2θ ½ |
| --- | --- | --- | --- | --- | --- |
|  |  | Min. | Typ. | Max. |  |
| Warm White | PO-MT3535WW-D01 | 2580 | / | 3710 | 120∘ |

Note:

- Maintains a tolerances of ±5% for CCT measurements.

- Electrical Characteristics

Ta=25℃）

| Color | Part No. | Forward Voltage VF(V) |  |  | Condition |
| --- | --- | --- | --- | --- | --- |
|  |  | Min | Type | Max |  |
| Warm White | PO-MT3535WW-D01 | 2.9 | / | 3.6 | IF=350mA |

Note:

1.  Maintains a tolerance of ±1v on Forward Voltage measurements.

- Bin Range Of Luminous Intensity

| Bin | Min | Max | Unit | Condition |
| --- | --- | --- | --- | --- |
| AA | 80 | 90 | lm | IF=350mA |
| AB | 90 | 100 |  |  |
| AC | 100 | 110 |  |  |
| AD | 110 | 120 |  |  |
| AE | 120 | 130 |  |  |

- Bin Range Of Forward Voltage

| Bin | Min | Max | Unit | Condition |
| --- | --- | --- | --- | --- |
| H1 | 2.9 | 3.0 | V | IF=350mA |
| H2 | 3.0 | 3.1 |  |  |
| I1 | 3.1 | 3.2 |  |  |
| I2 | 3.2 | 3.3 |  |  |
| J1 | 3.3 | 3.4 |  |  |
| J2 | 3.4 | 3.5 |  |  |
| K2 | 3.5 | 3.6 |  |  |

- Typical Electro-Optical-Thermal Characteristics Curves

(TA=25℃ Unless Otherwise Noted)

| 1.Relative Luminous Flux vs. Forward Current | 2.Forward Voltage vs. Forward Current |
| --- | --- |
| 3.Relative Luminous Flux vs. Ambient Temperature | 4.Forward Voltage vs. Ambient Temperature |
| 5.Spectrum Distribution-CRI 80 | 6. Radiation Diagram |

- ANSI Chromaticity Bin Table

Warm White BIN Structure

Note :The red dashed circle is main bin

| Bin code | CIE-x | CIE-y |  | Bin code | CIE-x | CIE-y |  | Bin code | CIE-x | CIE-y |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 35A | 0.3889 | 0.3690 |  | 30A | 0.4147 | 0.3814 |  | 27A | 0.4373 | 0.3893 |
|  | 0.3943 | 0.3853 |  |  | 0.4223 | 0.3990 |  |  | 0.4468 | 0.4077 |
|  | 0.4083 | 0.3921 |  |  | 0.4345 | 0.4033 |  |  | 0.4578 | 0.4104 |
|  | 0.4018 | 0.3752 |  |  | 0.4260 | 0.3854 |  |  | 0.4483 | 0.3919 |
| 35B | 0.3943 | 0.3853 |  | 30B | 0.4223 | 0.3990 |  | 27B | 0.4468 | 0.4077 |
|  | 0.3996 | 0.4015 |  |  | 0.4299 | 0.4165 |  |  | 0.4562 | 0.4260 |
|  | 0.4148 | 0.4090 |  |  | 0.4431 | 0.4213 |  |  | 0.4688 | 0.4290 |
|  | 0.4083 | 0.3921 |  |  | 0.4345 | 0.4033 |  |  | 0.4578 | 0.4104 |
| 35C | 0.4083 | 0.3921 |  | 30C | 0.4345 | 0.4033 |  | 27C | 0.4578 | 0.4104 |
|  | 0.4148 | 0.4090 |  |  | 0.4431 | 0.4213 |  |  | 0.4688 | 0.4290 |
|  | 0.4299 | 0.4165 |  |  | 0.4562 | 0.4260 |  |  | 0.4813 | 0.4319 |
|  | 0.4223 | 0.3990 |  |  | 0.4468 | 0.4077 |  |  | 0.4703 | 0.4132 |
| 35D | 0.4018 | 0.3752 |  | 30D | 0.4260 | 0.3854 |  | 27D | 0.4483 | 0.3919 |
|  | 0.4083 | 0.3921 |  |  | 0.4345 | 0.4033 |  |  | 0.4578 | 0.4104 |
|  | 0.4223 | 0.3990 |  |  | 0.4468 | 0.4077 |  |  | 0.4703 | 0.4132 |
|  | 0.4147 | 0.3814 |  |  | 0.4373 | 0.3893 |  |  | 0.4593 | 0.3944 |

Note:

Maintains a tolerances of ±0.01 on Color coordinates measurements.

- PACKAGING

PO-MT3535XXXX-X01 High Power LEDs are packaged in reel of 1000 pcs and placed inside a carton.

LABEL

BIN CODE

Lot

Qty

LABEL

BIN CODE

Lot

Qty

Carton

CARTON